## Slide 1
Hetero GNNs for defects
Low-to-high generalization in 2DMD
WU Hao
Group meeting 2026/9/15
Notes: 这次汇报接着之前的异构图工作，重点收敛到 2DMD 的低缺陷浓度训练、高缺陷浓度测试。首先说明数据与评估口径，然后介绍共享关系参数和逐缺陷能量读出，再讨论材料差异、超图消融和可复现性。日期按本次整理日期填写，可按实际组会日期修改。
Sources
C:/Users/User/Desktop/group meeting 20250805.pptx

## Slide 2
Recap: limited low-to-high transfer
Historical results from supplied training logs. Remote checkpoint configuration was not verified.
2
Lower low-val MAE, yet 2.51× the high-test error of attention.
Previous MoS₂ low-to-high runs. MAE in eV/defect.
Motivation for the current changes
Shared core + adapters: train the message core using all four relations.
Energy mean readout: predict each defect contribution before averaging.
Separate ablations are needed to determine the contribution of each change.
Previous model | Best low-val MAE | High-test MAE
ALIGNN attention | 0.002183 | 0.051590
ALIGNN hetero, independent | 0.001807 | 0.129310
Notes: 开场先回顾问题：之前的 hetero 并没有达到我们希望的 low-to-high 泛化效果。这一页引用的是同一材料 MoS₂ 的两份用户提供的完整训练 history，用户明确第一份为 attention，第二份为 hetero。hetero 目录为 features_layernorm/pool_defect_mean，对应当时尚未引入关系共享的版本。这里展示历史记录，不与后文 mixed-low 的当前结果拼成单因素消融。该远端 checkpoint 的内部配置和逐样本预测尚未核验，图上保留这一来源限制。
attention 的最佳 low 验证 MAE 为 0.002183，最终记录的 high 测试 MAE 为 0.051590。hetero 的最佳 low 验证 MAE 更低，为 0.001807，但 high 测试 MAE 达到 0.129310，是 attention 的 2.5065 倍。最重要的观察是：low 域拟合得更好，并没有带来更好的高缺陷浓度外推。两者都在最佳验证 epoch 后继续运行了 50 个 epoch，因此已有日志没有明显支持单纯训练不足的解释。
这引出后面的设计改动。第一，旧 hetero 的四种关系各有一套消息主体。对本地 MoS₂ 物理图的统计显示，low 中 defect–defect 邻居稀少，而 high 中明显增多。这使我们提出一个待检验假设：关系完全独立可能限制稀有关系的数据利用。于是引入每层共享消息主体，再用小型 relation adapter 保留关系差别。共享核心可以从所有四种关系的训练消息中学习，是否改善泛化仍需消融检验。
第二，另行检验读出：原来先平均实际缺陷的 latent representation，再通过非线性 MLP。现在让同一个 MLP 先对每个实际缺陷输出一个标量，再对这些标量求均值。目标仍是平均缺陷形成能，只使用图级标签，逐缺陷贡献不具有唯一真实能量的含义。这一步与参数共享是两个不同改动，应分别判断贡献。
过渡讲稿：所以今天的内容从这个泛化差距出发，先介绍共享消息主体与关系 adapter，再介绍逐缺陷预测后求平均的读出，随后展示结果和仍然存在的高浓度误差。原有图、节点类型融合以及其他具体保留的模块在后面的公式和备注中说明。
Sources
C:/Users/User/Desktop/HERA/logs/hetero_validation/supplied_remote_history_comparison.json
C:/Users/User/Desktop/HERA/docs/hetero_relation_shift_review.md
C:/Users/User/Desktop/HERA/docs/hetero_alignn_shared_relations.md
C:/Users/User/Desktop/HERA/docs/hetero_defect_energy_mean.md

## Slide 3
2DMD data and prediction target
Counts below describe each raw MoS₂/WSe₂ material subset. Mixed-low preprocessing retains 11,864 structures.
3
Target: y = Eformation / Ndefects
Low-density data | Structures per material
1 defect | 4
2 defects | 127
3 defects | 5,802
Total | 5,933
High-density data | Structures per material
4, 9, 14, 19, 24 defects | 100 at each count
Total | 500
97.8% of low structures have exactly 3 defects.
Notes: 预测目标核对为 formation_energy 除以缺陷数量，单位是 eV/defect，不是对所有原子平均。每种材料的 low 原始数据有 5933 条，其中 5802 条恰好 3 个缺陷，占约 97.8%。high 包含 4、9、14、19、24 个缺陷，每组 100 条。低浓度验证误差小只能说明 low 域拟合好，不能代表模型已经学会高浓度相互作用。mixed-low 经预处理保留 11864 条，和两个原始 low 子集简单相加的 11866 条有区别。
Sources
C:/Users/User/Desktop/HERA/logs/hetero_validation/wse2_evaluation_findings.md
C:/Users/User/Desktop/HERA/logs/hetero_validation/audit_mixed_vs_single_wse2.json

## Slide 4
Evaluation protocols
Checkpoint selection and learning-rate scheduling use validation data from the training domain.
4
Experiment | Training / validation | Test set
Low-domain benchmark | Mixed MoS₂ + WSe₂ low 7,118 / 2,373 | Held-out low: 2,373
High-domain benchmark | Six-material high 1,800 / 600 | Held-out high: 600
Single-material transfer | One material low 4,746 / 1,187 | Same material high: 500
Mixed-material transfer | Mixed low checkpoint Same low split as above | MoS₂ high: 500 WSe₂ high: 500
Low-domain MAE and low-to-high MAE answer different questions.
Notes: 这里有四种口径，必须分开。low benchmark 的 test 仍然来自 low；high benchmark 在包含六种材料的 high 数据中做域内划分。single-material 是某一种材料的 low 训练，测试同一材料的全部 high。mixed-material 使用混合 MoS₂/WSe₂ low 训练的一份模型，分别测试两个材料的 high，不包括另外四种训练未见材料。所有 checkpoint 都按训练域验证集选择。最近反复查看 high 来提出模型修改，因此 high 已参与开发反馈，后续更强的泛化结论需要冻结实验设置并增加独立外部验证。
Sources
C:/Users/User/Desktop/HERA/logs/hetero_validation/audit_mixed_vs_single_wse2.json
C:/Users/User/Desktop/HERA/logs/hetero_energy_mean_benchmark/high_test_predictions_fp32/low_to_high_analysis.json
C:/Users/User/Desktop/HERA/logs/hetero_energy_mean_benchmark/alignn/summary.txt
C:/Users/User/Desktop/HERA/main.py

## Slide 5
Models compared in the current study
Architectures below refer to the HERA implementations. These comparisons change more than pooling.
5
Model | Graph / messages | Readout
MEGNet sparse | Defect-only graph, 12 Å Current + original species Max in message/state blocks | Node + edge Set2Set and global state
ALIGNN attention | Atom/bond-angle graph, 6 Å Type-aware neighbor attention Shared message network | Type- and context-aware global attention
Shared ALIGNN hetero | Four directed relation types One message core per layer Rank-8 relation adapters | Mean of per-defect scalar predictions
DefiNet-style ALIGNN | Marker-pair and distance gates Scalar branch implemented in HERA | Mean over all nodes, then MLP
Notes: 这里避免把 sparse、attention 和 hetero 当成只差一个 pooling 的模型。sparse 使用 MEGNet 的缺陷图和 12 Å 距离，输入包含当前及原位元素，块内用了 max，但最终读出是节点和边的 Set2Set 再加全局状态。attention 和 hetero 使用 ALIGNN 的距离与角度主干，通常 cutoff 6 Å。attention 用节点类型参与局部与全局注意力，hetero 则保留四种关系，并共享消息主体。HERA 的 DefiNet 是标记对门控的 scalar 实现，不应当称为原论文所有分支的完整复现。
Sources
C:/Users/User/Desktop/HERA/models/alignn.py
C:/Users/User/Desktop/HERA/models/modules.py
C:/Users/User/Desktop/HERA/config
C:/Users/User/Desktop/HERA/logs/hetero_validation/compare_mos2_sparse_config.json

## Slide 6
Shared hetero: previous and current formulas
Each layer has its own weights. Superscript r denotes relation-specific weights.
Edge indices and affine biases are omitted. Relation-wise aggregation is unchanged.
6
r ∈ {pristine–pristine, defect–defect, pristine–defect, defect–pristine}
[δzᵣ, δvᵣ] = σ(aᵣ) Bᵣ SiLU(Aᵣ [hⱼ, hᵢ, eᵢⱼ])
zᵣ = Wₛʳhⱼ + Wₜʳhᵢ + Wₑʳeᵢⱼ
W: shared across relations. Aᵣ, Bᵣ, aᵣ: relation-specific. Bottleneck = 8.
Independent | Shared | Shared + rank-8 adapters
916,289 parameters | 614,465 parameters | 679,193 parameters
Previous: independent cores
Current: shared core + adapters
z = Wₛhⱼ + Wₜhᵢ + Wₑeᵢⱼ
mᵣ = σ(zᵣ) ⊙ Wₘʳhⱼ
mᵣ = σ(z + δzᵣ) ⊙ (Wₘhⱼ + δvᵣ)
Notes: 这页左侧是之前的 independent，右侧是当前实验的 shared_residual，不应把纯 shared 与当前基线混为一谈。
对一条 j→i、关系为 r 的边，旧版完整公式（省略层指标）是：z_ij^r = W_s^r h_j + W_t^r h_i + W_e^r e_ij + b_z^r，v_ij^r = W_m^r h_j + b_m^r，m_ij^r = sigmoid(z_ij^r) ⊙ v_ij^r。四种关系各自有一套完整参数。
当前版本：z_ij = W_s h_j + W_t h_i + W_e e_ij + b_z，v_ij = W_m h_j + b_m，[delta_z_ij^r, delta_v_ij^r] = sigmoid(a_r) [B_r SiLU(A_r [h_j,h_i,e_ij] + b_A,r) + b_B,r]，m_ij^r = sigmoid(z_ij + delta_z_ij^r) ⊙ (v_ij + delta_v_ij^r)。slide 中省略了边指标和 affine biases，W_s/W_t/W_e/W_m 统称 W。
同一层的四种关系共享 W。每种关系各有 A_r、B_r、a_r，同一关系内所有边共用该 adapter。不同层之间不共享。隐层 H=64，adapter 为 192→8→128，128 维分为 64 维 gate 修正和 64 维 value 修正。B 的权重和 bias 零初始化，a 初值 -3，因此初始残差为 0。
聚合公式没有改变：M_i^r = [sum_{j in N_r(i)} m_ij^r] / [sum_{j in N_r(i)} sigmoid(z_ij^r, effective) + 1e-6]，逐通道相除。各关系分别归一化，再按节点类型拼接关系槽做融合。不是所有关系的边共同做一次 softmax。边状态仍按 e'_ij = e_ij + SiLU(LN(z_ij^r, effective)) 更新。
节点类型 embedding、四套初始距离编码、节点类型融合仍有区别。参数数目沿用该 PPT 原来的同宽度对照：independent 916289，shared 614465，shared_residual 679193。只把四套消息主体改为共享不能消除所有关系差别。
Sources
C:/Users/User/Desktop/HERA/models/alignn.py (HeteroRelationConv, RelationResidualAdapter, SharedHeteroRelations, _hetero_relation_update)
C:/Users/User/Desktop/HERA/docs/hetero_alignn_shared_relations.md

## Slide 7
Defect readout: previous and current formulas
Readout is a separate change from relation sharing. Individual scalar contributions have no per-defect labels.
7
Previous: defect_mean
ŷ = g((Σᵢ hᵢ) / N)
Average defect representations,
then apply the nonlinear head g.
Current: defect_energy_mean
ŷ = (Σᵢ g(hᵢ)) / N
Apply the same head g to each defect,
then average the scalar predictions.
i ∈ D, where D contains actual defects and N = |D|.
Same MLP: 64 – 64 – 32 – 1. Same graph-level loss.
For nonlinear g, averaging and prediction generally do not commute.
Notes: 这里是另一个独立于参数共享的改动。之前的 defect_mean 为 y_hat = g((1/N) sum_{i in D} h_i)，当前实验使用的 defect_energy_mean 为 y_hat = (1/N) sum_{i in D} g(h_i)。D 只包含真实缺陷，N=|D|，所有缺陷使用同一个非线性 MLP g。g 的层宽仍然是 64→64→32→1，参数形状没有改变。代码默认值与具体实验配置要分开理解：本页“当前”指本 PPT 的当前实验配置。
非线性 g 通常不与 mean 交换。旧版先把所有缺陷的 latent representation 混合再预测，新版保留逐缺陷的非线性映射，最后对标量平均。h_i 已经包含环境和其他节点传来的消息，因此 pristine 节点仍间接影响读出。只在图级输出上逆变换 scaler 一次，图级目标仍是平均缺陷形成能。
逐缺陷标量没有单独监督，不能解释为唯一真实的逐缺陷形成能。该读出与 relation sharing 是两个改动，需要分别做消融才能确定各自贡献。
Sources
C:/Users/User/Desktop/HERA/models/alignn.py (HeteroALIGNN readout)
C:/Users/User/Desktop/HERA/docs/hetero_defect_energy_mean.md

## Slide 8
Mixed-low training: high-test results
Same 500 test IDs and targets per material. Historical baselines use earlier training versions / precision.
8
Chart: MAE (meV/defect)
| MoS₂ high | WSe₂ high
Sparse, historical | 136.3653 | 113.7406
Attention, historical | 96.6568 | 106.5368
Hetero, historical | 179.6383 | 59.7721
Shared hetero, current | 45.5356 | 59.0546
Current model: MoS₂ 45.54 meV/defect, WSe₂ 59.05 meV/defect
Notes: 这页所有模型都用 mixed low 训练。当前共享 hetero 通过一份最佳 epoch 303 的 checkpoint 分别预测两个 high 子集，用 FP32、batch 1。历史 baseline 已核对测试 ID 和标签一致，但没有统一代码和精度重训，因此只做历史结果比较。MoS₂ 相对旧 hetero 从 179.64 降至 45.54 meV，改善约 74.7%；WSe₂ 从 59.77 降至 59.05，基本相近。不能将当前结果直接宣称为所有配置下都优于 attention 或 sparse，更不能与单材料训练结果混为一组。
Sources
C:/Users/User/Desktop/HERA/logs/hetero_energy_mean_benchmark/high_test_predictions_fp32/low_to_high_analysis.json

## Slide 9
Error grows with defect count
Current mixed-low shared hetero. Each point contains 100 high-density structures per material.
9
Chart: Defects per structure
| 4 | 9 | 14 | 19 | 24
MoS₂ | 17.6443 | 26.7165 | 37.9113 | 59.9306 | 85.4754
WSe₂ | 9.0738 | 27.52 | 56.6604 | 80.8309 | 121.188
Chart: Defects per structure
| 4 | 9 | 14 | 19 | 24
MoS₂ | -15.761 | 16.0079 | 27.7939 | 56.1364 | 83.5546
WSe₂ | 4.5152 | 1.0616 | 43.5254 | 71.5858 | 116.6162
At 24 defects, mean bias is +83.6 meV on MoS₂ and +116.6 meV on WSe₂.
Notes: 将 500 条 high 按缺陷数分组后，误差随数量增加明显上升。4 个缺陷时 WSe₂ 比 MoS₂ 更低，但到了 24 个缺陷时 WSe₂ 达到 121.19 meV。右图定义偏差为预测减真实。24 缺陷时 MAE 与正偏差非常接近，说明误差主要由系统性高估构成，单纯增加优化轮数并不能直接针对这一现象。数据支持高浓度泛化是主要限制，但还不能唯一确定是几何交互、关系频率还是表示和读出的相关性造成。
Sources
C:/Users/User/Desktop/HERA/logs/hetero_energy_mean_benchmark/high_test_predictions_fp32/low_to_high_analysis.json

## Slide 10
Single-material rankings differ
High-test MAE, eV/defect. Seed 123. *MoS₂ shared hetero: supplied history, checkpoint not verified locally.
10
Each model trains on the low subset of its test material.
Model | MoS₂ high | WSe₂ high
MEGNet sparse | 0.161786 | 0.036967
ALIGNN attention | 0.056992 | 0.046233
Shared hetero + energy mean | 0.036838* | 0.052188
MoS₂: shared hetero has the lowest reported error in this comparison.
WSe₂: sparse and attention remain better than the current hetero.
Notes: 这页改为单材料训练口径，不能与上一页 mixed-low 混合排名。MoS₂ 的新 hetero 0.036838 来自用户贴出的训练 history 和明确的实验目录，该 checkpoint 尚未本地核对，标星展示。WSe₂ 新 hetero checkpoint 已下载，保存的 test MAE 为 0.052188；它仍比 sparse 0.036967、attention 0.046233 大。旧版 WSe₂ sparse、attention、hetero 的全 high 复核保留了排序，因此目前没有证据说明优势来自简单的测试集读错。但该比较没有固定 backbone、特征与所有训练条件，不能把差异唯一归于材料本身。
Sources
C:\Users\User\.codex\attachments\40916e91-6e79-4164-b78f-70d54f1072a5\pasted-text.txt
C:/Users/User/Desktop/HERA/logs/hetero_energy_mean_benchmark/alignn/summary.txt
C:/Users/User/Desktop/HERA/logs/hetero_validation/wse2_evaluation_findings.md
C:/Users/User/Desktop/HERA/docs/hypergraph_v3_completed_diagnosis.md
C:/Users/User/Desktop/HERA/logs/hetero_validation/compare_mos2_sparse_retest_history.json

## Slide 11
Mixed and single-material training differ
Same WSe₂ high test set. Training composition and the number of WSe₂ training examples both change.
11
Chart: MAE (meV/defect)
| Sparse | Attention | Shared hetero
Mixed low training | 113.7406 | 106.5368 | 59.0546
WSe₂-only low training | 36.9666 | 46.2329 | 52.1885
WSe₂ training samples: 3,588 in mixed low versus 4,746 in WSe₂-only low.
Material interference is a hypothesis. Historical model versions also differ.
Notes: 同样在 WSe₂ high 上，mixed-low sparse 与 attention 的历史结果比单材料训练差很多。一个明确的混杂因素是 mixed 60/20/20 划分只用了 3588 条 WSe₂ 训练结构，而单材料 80/20 划分用了 4746 条 WSe₂。也存在历史版本不同，例如 mixed attention 的旧 BN 与单材料较新配置。因而不能直接归因于负迁移。更可靠的对照是保持相同 WSe₂ 训练 ID，再加入 MoS₂ 数据，并匹配总优化步数、材料采样与 checkpoint 选择。当前 shared hetero 的 mixed 和 single WSe₂ 差距较小，但仍只有单 seed。
Sources
C:/Users/User/Desktop/HERA/logs/hetero_validation/audit_mixed_vs_single_wse2.json
C:/Users/User/Desktop/HERA/logs/hetero_energy_mean_benchmark/high_test_predictions_fp32/low_to_high_analysis.json
C:/Users/User/Desktop/HERA/logs/hetero_energy_mean_benchmark/alignn/summary.txt

## Slide 12
Hypergraph results depend on the version
MoS₂ low-to-high, seed 123. Different rows change readout and sometimes other architecture components.
12
Version | Readout | High MAE (eV/defect)
Original attention reference | Global attention | 0.056992
Hypergraph v2 | Earlier hierarchical readout | 0.168732
Hypergraph v3, earlier run | Hierarchical attention | 0.250031
Hypergraph v3, later run | Defect mean, local + global | 0.068386
The 0.25 and 0.068 results belong to different trained models.
A better readout does not establish a benefit from hypergraph messages.
Notes: 之前以为结果在 0.1 左右，后来看到 0.25 或 0.06，关键是版本不一致。v2 为 0.168732；旧 v3 使用分层 attention 读出，checkpoint 的预测头输入 256 维，结果 0.250031。后来的 defect_mean 去掉额外背景读出分支，预测头输入 64 维，重新训练的 local+global 为 0.068386。不能将推理时临时换 pooling 的实验解释为新版本训练成绩，也不能把不同版本所有改善都归因于唯一因素。接下来用同一版本的更新消融判断超边消息是否有贡献。
Sources
C:/Users/User/Desktop/HERA/docs/hypergraph_v3_completed_diagnosis.md
C:/Users/User/Desktop/HERA/logs/2dmd_mos2_hypergraph_ablation/alignn/2dmd_mos2/summary.txt

## Slide 13
Hypergraph updates: matched ablation
All MAEs: meV/defect. Fixed v3, defect mean, seed 123. “None” retains the HyperALIGNN backbone.
13
Chart: MAE (meV/defect)
| No hypergraph update | Local only | Local + global
High test | 61.9407 | 75.8231 | 68.386
Update | Low val MAE
None | 2.066
Local | 2.313
Local + global | 2.239
Neither enabled update improves on “none” in this run.
Notes: 这三组才是当前相对明确的超图消息对照，物理主干、读出和初始权重一致。关闭整个超图更新块为 0.06194，local 0.07582，local+global 0.06839。global 相对 local 减少了一部分误差，但仍然没超过关闭更新。这个结果不支持“local 永远没用”，也不能评价尚未完成的 global-only 或 energy-mean 组合。当前局部超边由中心 defect 和 3 Å 内 pristine 构成，不包含其他 defect；全局超边连接全部 defects，没有直接输入成对的 defect 距离。单 seed 结果需要复验。
Sources
C:/Users/User/Desktop/HERA/docs/hypergraph_update_ablation.md
C:/Users/User/Desktop/HERA/docs/hypergraph_energy_global_ablation.md
C:/Users/User/Desktop/HERA/logs/2dmd_mos2_hypergraph_ablation/alignn/2dmd_mos2/summary.txt

## Slide 14
Reproducibility and training sensitivity
MAE: eV/defect. Short-run numerical differences do not explain the full historical accuracy gap.
14
MoS₂ sparse run | Best low val MAE | High MAE
Local saved run | 0.002972 | 0.161786
New supplied run | 0.002466 | 0.192789
Lower low-domain validation error accompanied worse high-domain error.
Independent-process audit | Finding
Fixed checkpoint inference | Exact across repeat GPU runs
100 training steps on GPU | First gradient differs by up to 7.45 × 10⁻⁹
100 training steps on CPU, 1 thread | Exact repeat
Notes: MoS₂ sparse 新跑出的 high 误差比本地记录高约 19.2%，虽然 low 验证更好。已确认本地旧 checkpoint 与当前 sparse 默认配置和参数形状匹配，但新远端权重与环境未完全核对，不能断言两次一切相同。独立进程短测试固定了代码、环境、图、初始化和 batch 顺序。GPU 固定权重推理完全一致，第一步梯度开始出现约 7.45e-9 的差异，100 步后最大预测差约 1.86e-5；CPU 单线程完全一致。这证明训练数值可重复性有限，不能证明这么小的差异必然导致历史 0.03 的 MAE 差。后续要记录代码、环境和划分并跑多 seed。
Sources
C:/Users/User/Desktop/HERA/logs/hetero_validation/compare_mos2_sparse_retest_history.json
C:/Users/User/Desktop/HERA/logs/hetero_validation/compare_mos2_sparse_config.json
C:/Users/User/Desktop/HERA/logs/sparse_reproducibility/20260915_021549_556655/report.json

## Slide 15
Next controlled hetero experiments
Implemented options. Full low-to-high accuracy results are not yet available locally.
15
Variant | Single intended change | Question tested
Current baseline | Shared + rank-8 adapters Energy mean readout | Reference result
Cross-relation attention | Normalize gate logits across all incoming relations | Does relation-wise normalization lose useful competition?
Sparse residual | Add 12 Å defect–defect messages Distance RBF + ordinary mean Zero-initialized output projection | Does direct defect geometry help at higher density?
Compare each change separately with the same split and initialization.
A zero initial residual matches the baseline initially, but gives no accuracy guarantee.
Notes: 当前基线已经完成结果分析。下一步两个选项都已实现，但没有本地完整训练结果。跨关系注意力复用 gate logits，对同一目标的所有关系入边统一逐通道 softmax，仍保留关系消息槽。它不是原 attention 的四头网络完全复制。sparse residual 在主干读出之前加入 12 Å 的真实缺陷间消息，使用距离 RBF 和 gated message，按照用户确定的普通 mean 聚合，不能写成 max。输出投影从零初始化，因此初始模型与 baseline 完全相同。优先分开测试，避免把多个改动叠加后无法解释。
Sources
C:/Users/User/Desktop/HERA/docs/hetero_interaction_ablation.md
C:/Users/User/Desktop/HERA/models/alignn.py

## Slide 16
Full benchmark protocol
Prepared command and inference support. The complete benchmark has no new local result table yet.
16
Stage | Coverage | Output
1. Domain benchmarks | CGCNN, MEGNet, ALIGNN All supported modes on low and high | 32 modes × 2 datasets 64 training runs at seed 123
2. Low-to-high evaluation | Load only 2dmd_low checkpoints Evaluate MoS₂ and WSe₂ separately | 32 models × 2 materials Per-model predictions and MAE
3. Stability follow-up | Repeat selected comparisons with multiple fixed seeds | Mean ± standard deviation Error and bias by defect count
Freeze the protocol before interpreting the final model ranking.
“All” includes supported WAS variants. Duplicate hetero fixed-pool r=0 is skipped.
Notes: 已经补齐 main 与 low checkpoint 推理脚本。all 覆盖三个 backbone 的适用模式，共 32 个非重复配置，两个数据集合计 64 组 seed123 训练。训练完只筛选 low 权重，在 MoS₂ high 和 WSe₂ high 分开测试，每个 500 条。high 域内 benchmark 则包含六种材料，不能与这两个子集混淆。当前命令是单 seed，不能生成有意义的 seed 方差；多 seed 是下一步。也要明确，各 backbone 保留适用的原配置，这是一组 benchmark，不是每一项都属于单因素消融。
Sources
C:/Users/User/Desktop/HERA/README.md
C:/Users/User/Desktop/HERA/main.py
C:/Users/User/Desktop/HERA/predict_2dmd_low_checkpoints.py
C:/Users/User/Desktop/HERA/tests/test_predict_2dmd_low_checkpoints.py

## Slide 17
Conclusions and next steps
Current conclusions are limited to the available configurations and seed-123 runs.
17
Shared hetero is a stronger current baseline
Mixed-low high MAE: MoS₂ 0.04554, WSe₂ 0.05905 eV/defect.
Dense-defect generalization remains unresolved
The residual error increasingly reflects positive bias as defect count rises.
The next decision needs matched experiments
Finish the all-model benchmark, then compare relation attention and
distance-based defect residuals with repeated seeds.
Notes: 收束到三个结论。第一，共享消息主体、关系 adapter 和能量均值读出形成了目前更强的 hetero 基线，尤其是 mixed-low 的 MoS₂，但单材料 WSe₂ 仍未超过 sparse 和 attention。第二，主要剩余问题是高浓度正偏差，不能只追求更低的 low 验证误差。第三，超图更新没有显示额外收益，应先完成可追溯的全模型 benchmark，再做跨关系 attention 和距离缺陷残差的独立实验，用多 seed 判断提升是否稳定。这里不承诺任何一个结构一定超过 attention。
Sources
C:/Users/User/Desktop/HERA/logs/hetero_energy_mean_benchmark/high_test_predictions_fp32/low_to_high_report.md
C:/Users/User/Desktop/HERA/logs/2dmd_mos2_hypergraph_ablation/alignn/2dmd_mos2/summary.txt
C:/Users/User/Desktop/HERA/docs/hetero_interaction_ablation.md

## Slide 18
Appendix: attention architecture
Mechanistic interpretation below is a hypothesis about generalization, not a controlled causal result.
18
Local message and neighbor weighting
uᵢⱼ = sigmoid(G[hᵢ,hⱼ,eᵢⱼ]) ⊙ MLP([hᵢ,hⱼ,eᵢⱼ])
αᵢⱼ = mean of 4 head-wise neighbor softmax weights
Global readout
βᵢ = softmaxᵢ(score[hᵢ, typeᵢ, meanⱼ hⱼ])
ŷ = MLP(Σᵢ βᵢ hᵢ)
Shared messages, neighbor competition and learned defect emphasis may help transfer.
Notes: 默认配置是 hidden64、3 个 attention ALIGNN block 加 3 个 GCN block，后接类型和全局上下文条件的 attention 读出。局部消息同时看源、目标和边特征，并有 sigmoid gate；注意力打分再额外看两个端点类型。四个 head 分别对邻居归一化，最后平均权重乘同一条消息，不是标准 Transformer 把四套 value 拼接。全局 score 同时看 h_i、类型 embedding 和全图平均上下文。共享参数和邻居竞争是值得借鉴的机制，但不能从性能排名证明它们就是泛化提升原因，也不能把注意力权重当作因果重要性。
Sources
C:/Users/User/Desktop/HERA/models/alignn.py
C:/Users/User/Desktop/HERA/models/modules.py

## Slide 19
Appendix: adapters and DefiNet-style gates
The current baseline uses a linear source-message projection plus relation adapters.
19
Component | Conditioning | Role
Hetero relation adapter | Source, destination and edge state One adapter per relation per layer | Corrects both gate logits and message values
DefiNet-style gate | Marker-pair embedding with separate distance modulation | Reweights a shared message without neighbor softmax
Pair-message option | MLP([source, destination, edge]) | Makes the shared value explicitly pair-conditioned
Shared-distance option | Shared RBF encoder with zero-initialized relation offsets | Reduces independent relation-distance encoders
Pair-message and shared-distance options need separate performance tests.
Notes: 用户之前关心 adapter 和 DefiNet 是否一样。两者都利用类型信息，但参数化不同。adapter 是每层、每关系一套根据源目标边状态计算的低秩修正，同时改变 gate 和 value；DefiNet-style scalar 门控根据标记对和距离调制共享消息，不等同四个独立关系修正网络。前面还实现过 pair_message 与 shared_distance 选项。当前带正式结果的基线没有同时开启这些选项，也没有启用下一轮的 cross_relation_attention 或 sparse_residual，因此报告不能把它们写成已有性能来源。
Sources
C:/Users/User/Desktop/HERA/docs/hetero_alignn_shared_relations.md
C:/Users/User/Desktop/HERA/docs/hetero_message_distance_ablation.md
C:/Users/User/Desktop/HERA/models/modules.py
C:/Users/User/Desktop/HERA/models/alignn.py

## Slide 20
Appendix: checkpoint and metric identity
All MAEs below use eV/defect. Paths, source tables and caveats are recorded in the speaker notes.
20
Saved model / evaluation | Best epoch | Test MAE
Mixed low, held-out low | 303 | 0.002633
Same mixed-low weights, MoS₂ high | 303 | 0.045536
Same mixed-low weights, WSe₂ high | 303 | 0.059055
Separate high-trained model, high-domain test | 214 | 0.052567
Separate WSe₂-low model, WSe₂ high | 243 | 0.052188
Shared hetero: r=0, LayerNorm, rank 8, defect_energy_mean
Mixed-low checkpoint SHA-256 begins aaf4995019b6dbe7
Notes: 这页用于追溯常见的数字混淆。0.002633 是 mixed-low 模型的 low 域内 test，不是 high；0.052567 是另一个用 high 训练的模型做 high 域内测试，不是 low-to-high。0.045536 和 0.059055 才来自同一份 mixed-low checkpoint 的两个外部 high 子集。shared hetero 的全程 LayerNorm、r0、rank8 和 energy mean 由 checkpoint config 核对。混合低浓度 checkpoint SHA256 为 aaf4995019b6dbe70d4da0c5aa65ff9eefead9f37e49f4b64c7cc1a048548a49。本次外部评估为 FP32、batch1、RTX5060Ti，500 条唯一 ID 和原始 high 标签已匹配。
Sources
C:/Users/User/Desktop/HERA/logs/hetero_energy_mean_benchmark/high_test_predictions_fp32/low_to_high_analysis.json
C:/Users/User/Desktop/HERA/logs/hetero_energy_mean_benchmark/alignn/summary.txt
C:/Users/User/Desktop/HERA/logs/hetero_energy_mean_benchmark/alignn/2dmd_high/hetero/r0/features_layernorm/pool_defect_energy_mean/relations_shared_residual_rank8/seed123_history.csv
C:/Users/User/Desktop/HERA/logs/hetero_energy_mean_benchmark/alignn/2dmd_wse2/hetero/r0/features_layernorm/pool_defect_energy_mean/relations_shared_residual_rank8/seed123_history.csv